Ti-Silicide 형성에 미치는 전세정 효과

정상철, 박지수, 윤여분, 노재성, 김재정

LG반도체 기반기술연구소

The Effect of Precleaning Treatments on The Formation of Ti-Silicide

Sang-Chul JUNG, Ji-Soo PARK, Yeo-Boon YOON, Jae-Sung ROH, Jae-Jeong KIM

Advanced Technology Laboratory of LG Semicon Company Limited

1. Introduction

Titanium silicide is widely used for contacts and interconnects in metal-oxide-semiconductor(MOS) integrated circuits because of its low resistivity and high temperature stability. A typical self-aligned-silicide (SALICIDE) process involves deposition of a thin film of  titanium onto a MOS transistor structure. A low temperature (≤730℃) anneal is then performed to induce silicidation over the gate and source/drain regions, followed by removal of the titanium over oxide regions using a selective wet etch. Finally, an 800~900℃ homogenization anneal completes the silicidation reaction and reduces the TiSi2 resistivity to about 15μΩ-cm. The silicide formation is generally affected by the metal/silicon interface state, and TiSi2 growth has the incubation time of silicide formation for the Ti/Si systems with the silicon oxide at the Ti/Si interface. Consequently, to be able to control the condition of Si surface is a critical issue, in order to form low resistance TiSi2 film on the Si surface. Thus, it is important to clarify the surface treatment effect before Ti deposition. In this work, the silicon surface treatments are investigated to from low resistance TiSi2 film. we investigated the effect of precleaning treatments include wet(APM, HPM, HF) and dry(Ar+ sputtering) cleaning.

Table 1. TiSi2 film formation process flow

| Process step | Conditions |
| --- | --- |
| surface treatment | Eleven sequences A-K |
| Ti deposition | 400Å |
| 1st RTP | 680, 700, 720℃, 20sec |
| selective Ti/TiN etching | APM chemical solution |
| 2nd RTP | 850℃, 20sec, in N2 gas |

2. Experimental

The titanium silicide formation sequence is shown in Table 1. Following the Ar dry precleaning treatment, 400Å Ti was deposited using in situ sputtering in a clustering tool. One of the Si-surface treatment sequences before the Ti deposition, summarized in Table 2, was carried out. The TiSi2 films were formed by the conventional 2-step rapid thermal annealing(RTA) process. Eleven sequences A-K, combined four surface treatments, before the Ti deposition, were evaluated for the Si-surface condition control to form low resistance

TiSi2 film. The HPM treatment makes thin chemical oxide film on the Si-surface. The APM treatment, HF dipping and Ar+ sputtering are used to remove the surface native oxide film. After the formation of TiSi2 film, the cross-section of TiSi2 was observed using a TEM, and the morphology was investigated by SEM and AFM. The sheet resistance was measured by the four probe method. The impurity depth profiles in TiSi2/Si system was analyzed by SIMS.

Table2. Si-surface treatment sequence

3. Results and Discussion

Figure 1 shows the sheet resistance dependence on surface treatment sequences. This sheet resistance was measured after the selective TiN etching. Sheet resistance of TiSi2 film treated by sequences H and I were higher than those treated by other sequences. Figure 2 shows the sheet resistance dependence on surface treatment sequences after the 2nd RTA. Sheet resistance of TiSi2 film treated by sequences H and I were the same higher than those treated by other sequences. To investigate the TiSi2 sheet resistance dependence on the Si surface treatment, impurity concentration in the TiSi2/Si structure and TiSi2 crystal structure were analyzed. SIMS depth profiles for silicon, oxygen, nitrogen and carbon in TiSi2 films treated by four surface cleaning are shown in Fig.3. A large peak of oxygen along with nitrogen appears in the Ar dry cleaning treated film. Since Ti is not able to reduce SiO2 under standard processing conditions, the presence of a native oxide on the Si surface, before Ti deposition, might influence the silicidation reaction. This may result in silicide-silicon interface roughness. This was investigated by TEM.

| Sequence | Treatment |
| --- | --- |
| A | No cleaning |
| B | APM(SC1, NH4OH : H2O2 : H2O) |
| C | HPM(SC2, HCl : H2O2 : H2O) |
| D | HF cleaning |
| E | APM + HPM |
| F | APM + HF |
| G | HPM + HF |
| H | APM + HPM + HF |
| I | Ar pre-cleaning (6sec) |
| J | APM + HPM + Ar pre-cleaning |
| K | HF + Ar pre-cleaning |
| L | APM + HPM + HF + Ar pre-cleaning |

Fig.1 Sheet resistance dependence on the 1st RTA

temperature after selective metal etching

Fig.2 Sheet resistance dependence on the 1st RTA

temperature after the 2nd RTA

Fig.3 SIMS depth profiles for silicon, oxygen, nitrogen and carbon in TiSi2 films,

after 2nd RTA at 850ꇉ with 1st RTA at 680ꇉ.

Fig.4 shows cross-sectional TEM images of the TiSi2/Si structure. Avery smooth interface is obtained when the wafers are given a HF dip immediately before loading in the sputtering chamber(Fig.4(a)). The interface treated Ar dry cleaning before the loading is hardly detectable increase roughness(Fig.4(b)). The higher sheet resistance of TiSi2 film treated by sequence H is explained by the interface roughness, than those treated by other sequences, shows in Fig.1,2.

Fig.4 Cross-sectional TEM micrograph of silicide layers after 2nd RTA at 850ꇉ

with 1st RTA at 680ꇉ.

4. Conclusions

We investigated the effect of precleaning treatments on the formation of TiSi2 in the SALICIDE process. The sheet resistance for thinner TiSi2 films strongly depends on the Si-surface treatment. The sheet resistance surface treatment dependence was explained by tee silicide formation suppression caused by the residual oxygen at the TiSi2/Si interface. SiLicide with an extremely smooth silicide-silicon interface and very low resistivity are obtained by wet cleaning process.

References

1. M.L. Polignano et.al., J. Appl. Phys., 68, 1869(1990)

2. T. Maeda et.al., IEEE Trans. Elec. Dev., ED-34, 599(1987)

3. W. Tsai et.al., IEEE Trans. Elec. Dev., Vol. 41, No. 8, p1396(1994).