열수축필름 제조를 위한 LLDPE/LDPE 블렌드

최석환, 황규면, 박인하

유공 대덕기술원 고분자연구1팀

LLDPE/LDPE BLENDS FOR HEAT SHRINKABLE FILMS

SUEK HWAN CHOI, K. M. HWANG , INHA PARK

YUKONG TAEDOK INSTITUTE OF TECHNOLOGY POLYMER LAB.I

INTRODUCTION

Shrink packaging is a relatively simple process by which products can be wrapped, bundled, palletized and displayed.

Films made from the high pressure low-density polyethylene by the bubble process shrink (up to 75% in MD) if they are heated without restraint. In addition, the low-density polyethylene film is one of the cost efficient polymer films. For this reason, the conventional blown shrink film market is dominated by low-density polyethylene.

Even though the LDPE’s are generally more expensive and relatively low physical properties than linear low density polyethylene (LLDPE), LLDPE is not used for heat shrinkable film application due to the poor shrink property of the LLDPE film. In this study, we explored the possibility of utilization of LLDPE in the shrink film applications as a blend with LDPE.

EXPERIMENTAL

Two low density polyethylene resins produced by HANHWA chemical co. were used ; 5301, 5602. These are typical LDPE resins for shrinkable film with melt indices of 0.3, 0.8, respectively and 0.920 density. Three ethylene-butene LLDPE resins produced by YUKONG LIMITED were tested ; FN400S, FN410, FV149M. These are typical blown film grades with melt indices of 0.6, 1.0, 1.8, respectively and 0.919 density. The LDPE/LLDPE  blends were prepared by dry blending. The blends of 50/50 LDPE and LLDPE by weight were mainly used for the shrink film in this study.

A single screw extruder with 50㎜ diameter, 24:1 L/D equipped with a 150㎜ die (2.0 ㎜ die gap) was used. Also, a 50㎜, 26:1 L/D single screw extruder with a 75 ㎜ die (1.0 ㎜ die gap) was used in studying the effect of blowup ratio(BUR) of the film.

The LDPE/LLDPE blending ratio, LDPE and LLDPE MI, blowup ratio, drawdown ratio, melt temperature (die lip temperature) and frost line height were systematically varied. Except the test of BUR and DDR effect, final film thickness and BUR were kept constant at 50㎛ and 2.7, respectively.

The tensile properties of films were measured by ASTM D-882. The evaluation of free film shrinkage was accomplished according to ASTM D-2732.

RESULTS AND DISCUSSION

The physical properties and shrinkage data of the films fabricated under various LDPE/LLDPE blending ratio are tabulated in Table 1. Table 1 shows that the tensile strength increases as the concentration of LLDPE increases and elongation decreases as concentration of LDPE increases.

Figure 1 shows, when the LDPE portion in the blends is between 30 and 70% by weight, the shrinkage of films is about 70 to 80% in MD and 10 to 20% in TD at a shrink temperature of 130 and 140℃.

Fig.1 Shrinkage vs. LLDPE/LDPE Blending Ratio

The usage of an LLDPE with a higher melt index results in a lower tensile strength of the films. However, the melt index of LDPE affect little on the tensile strength compared to LLDPE. The elongation of the films is affected by the melt indices of LDPE and LLDPE. A higher melt index results in higher elongation properties. A lower melt index of LLDPE or LDPE results in a higher shrinkage of films. The TD shrinkage of the films increases as the melt index of the blended LDPE decreases. However, the melt index of blending LLDPE is observed not so effective on the shrinkage of the film as the MI of LDPE.

Increasing BUR caused a higher TD orientation leading to a lower TD elongation and a higher TD shrinkage. However, a better correlation of TD shrinkage was obtained as a function of BUR/DDR as shown in Figure 2. This can be explained as TD shrinkage of a film is affected by the orientation in MD.

The effect of DDR in film was studied using films with different thickness and the die gap. BUR and screw r.p.m. were kept constant in this study. A higher DDR of a film results in a lower MD elongation. However, DDR of films does not have an appreciable effect on TD elongation.

Fig.2 Shrinkage vs. BUR/DDR

A plot of MD shrinkage as a function of DDR is shown in Figure 3. As we expected, a higher MD shrinkage was obtained at a higher DDR. However, TD shrinkage was not affected by DDR in the test condition.

The Die Lip Temperature has an effect on the shrinkage of the films. There were some evidences that the shrinkage decreased as the Die Lip Temperature increased. However, the effect of Die Lip Temperature was too small to consider in this Die Lip Temperature range.

Fig.3 Shrinkage vs. DDR

As the frost line height is increased the TD elongation is decreased and MD elongation is increased. However, TD shrinkage is increased and MD shrinkage is decreased as the Frost Line Height is raised. This is, most of the MD orientation is done near the die at higher melt temperature and TD orientation is done near the frost line at a cooler temperature.

Fig.4 Shrinkage vs. Frost Line Height

CONCLUSIONS

Shrinkage measurement shows that LDPE/LLDPE blend films have good shrink properties enough to be utilized commercially. The TD shrinkage of LDPE/LLDPE blend films is related to blowup ratio (BUR) and in particular to BUR/DDR. The MD shrinkage of blend films is connected with drawdown ratio (DDR). The MD and TD shrinkage are related to frost line height and melt temperature, also.

The MD and TD shrinkage ratio can be varied in accordance to the packaging applications. To satisfy the MD and TD shrinkage, the proportion  of LDPE in the blends with the LLDPE may be varied between 30 and 70% by weight. The films are to be fabricated at 1∼2 ㎜ die gap and BUR of 2.5 ∼ 4.0. The processing temperature and frost line height should be considered.

It is possible to use LDPE/LLDPE blends for an enhanced strength shrink film. A butene-copolymer LLDPE with MI=1.0 , ρ = 0.919 seems to be suitable to form a useful blend with LDPE because of the good physical properties of the LLDPE resin.

APPENDIX

Table 1. Tabulation of LDPE/LLDPE blending ratio of films 
and corresponding physical properties and shrinkage data.

| LLD/LD | LLDPE | 100 | 90 | 70 | 60 | 50 | 30 | 10 | 0 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| % | LDPE | 0 | 10 | 30 | 40 | 50 | 70 | 90 | 100 |
| Strength | MD | 350 | 330 | 320 | 300 | 300 | 310 | 280 | 260 |
| Kg/㎠ | TD | 350 | 340 | 320 | 320 | 310 | 300 | 250 | 240 |
| Elongation | MD | 700 | 650 | 590 | 530 | 460 | 280 | 320 | 330 |
| % | TD | 780 | 770 | 770 | 760 | 720 | 640 | 620 | 580 |
| Shrinkage | MD | 35 | 58 | 65 | 68 | 71 | 73 | 69 | 68 |
| @120℃,% | TD | -5 | -10 | 0 | 5 | 8 | 11 | 22 | 27 |
| Shrinkage | MD | 46 | 63 | 71 | 73 | 74 | 76 | 72 | 69 |
| @130℃,% | TD | -8 | -4 | 11 | 13 | 18 | 23 | 21 | 28 |
| Shrinkage | MD | 47 | 66 | 72 | 75 | 76 | 79 | 73 | 74 |
| @140℃,% | TD | -9 | -4 | 11 | 13 | 20 | 21 | 26 | 29 |

Table 2. Tabulation of melt index of blended LDPE and LLDPE and corresponding physical properties and shrinkage data of films.

| LLDPE | MI | 0.6 | 1.0 | 1.8 | 0.6 | 1.0 | 1.8 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| LDPE | MI | 0.3 | 0.3 | 0.3 | 0.8 | 0.8 | 0.8 |
| Strength | MD | 340 | 310 | 290 | 340 | 310 | 280 |
| Kg/㎠ | TD | 350 | 320 | 300 | 320 | 320 | 280 |
| Elongation | MD | 430 | 470 | 470 | 470 | 510 | 510 |
| % | TD | 680 | 700 | 700 | 720 | 740 | 730 |
| Shrinkage | MD | 68 | 67 | 68 | 69 | 67 | 68 |
| @120℃,% | TD | 15 | 13 | 12 | 8 | 7 | 8 |
| Shrinkage | MD | 77 | 77 | 77 | 76 | 75 | 75 |
| @140℃,% | TD | 19 | 17 | 17 | 13 | 15 | 13 |