³¿¼ Polyimide ¹¸À imidization history¿ thermal cycling¿ µ¸

residual stress °µ

Á Ç ¼, ¹ ¼ ±, À Ã È, Á ¿ À, Ç Ç ¼

¿¼´Ç± ÈÇ°Ç°

The Effect of Imidization History and Thermal Cycling on Residual Stress Behaviors in High Temperature Polyimide Thin Films

Hyun-Soo Chung, Sung-gook Park, Chang-ho Lim, Yung-il Joe, Hak-Soo Han

Dept. of Chemical Engineering, Yonsei University

Introduction

The current trend in the interconnect development is to incorporate polymer layers together with glass or ceramic layers to form a multilayered wiring structure. The use of polymers is, however, not without problems. One of the most important concerns is the mechanical integrity of the multilayered structures. For multilayered device, there are often reliability problems, such as displacement, cracks, and delamination at interfaces. Thermal stress cause interfacial adhesion and mechanical failures associated with interfacial residual stress due to the mismatch of physical properties between polymers and the other materials used. The mismatch in thermal expansion coefficient and the Young’s modulus will generate thermal stress in the metal/polymer structure during thermal cycling[1,2]. Since thermal cycling is a typical procedure during fabrication and polymer curing, it is important to understand the mechanical properties of the metal/polymer structure, particularly the nature of stress relaxation during thermal cycling.

Due to volatilization of different volume by-products during curing process, the morphological structure and chain rigidity of polyimide thin films can be changed. For this study, a computer-controlled experiment has been set up to measure the thermal stress of multilayered films using the bending wafer technique.		To understand and classify these phenomena, the bending beam  technique for thermal stresses kinetics according to Imidization history and thermal cycling in polyimide thin films prepared from various precursors was used.

Experimental

The different backbone structure polyimides; semi-flexible poly(4,4'-oxydipheylene pyromellitimide): PMDA-ODA, semi-rigid poly(p-phenylene biphenyltetracarboximide): (BPDA-PDA) were used  in this work. Two different amic acid precursor solutions; PMDA-ODA PAA(Mw 35,000  and 16.0 wt%) and  BPDA-PDA PAA(Mw 40,000 and 13.5 wt%) were synthesized in a N-Methyl-2-Pyrrolidone(NMP) through polymerization from the respective dianhydrides and diamines purified through recrystallization from our lab. In addition, two other poly(amic dialkyl ester) were synthesized and prepared via low temperature solution polycondensation in NMP of diethyl diacyl chloride with ODA and PDA. The prebaked samples were then placed in the curing oven at 80oC for 10 min and cured under flowing nitrogen by the following  cure schedule: 150oC for 30 min, 230oC for 30 min  300oC for 30 min, and 400oC for 60 min[3,4,5].

For all the one-side polished Si(100) wafers of 3 in diameter used in this study, curvatures were measured with the aid of a He-Ne laser beam based stress analyzer equipped with a hot-stage. A sample (film on cleaned silicon wafer) and a blank, 412(m-thick reference silicon wafer were mounted on a hot-stage. The curvature of the wafer was measured continuously by a computer-controlled system during thermal cycling. A position sensor was used to measure the position of the reflected He-Ne laser beam impinging on the surface of the wafer. The sensor was designed to read the position of the laser spot but was not sensitive to the laser spot size. A position sensor amplifier provided a voltage monitoring the position of the laser spot on the sensor. This voltage is normalized with respect to the laser light intensity such that its magnitude is not affected by the reflectivity change of the sample surface during thermal cycling. The output voltages of the position sensor amplifier were read using a digital converter and transferred to an IBM personal computer. The computer then converts the position voltage to the wafer curvature and also thermal stress behaviors for precursors and cured polyimide thin films were investigated geometrically. The experimental data were plotted with thermal stresses(() as a function of  Ef/(1-(f) is biaxial elastic modulus, ( is the thermal expansion coefficient of film and tf  is the thickness of film[6].

µ §                                    (1)

Using equation (1),  residual stresses of thin films were investigated

Results and Discussion

In Table 1, thermal induced stress results are given for different backbone structure polyimide films; PMDA-ODA, and BPDA-PDA. Prepared from amic acid and ester precursors, the BPDA-PDA polyimide film exhibits lower residual stresses during curing process, the PMDA-ODA polyimide film exhibits the reverse. It shows that the overall residual stress of a polyimide film is generated by the mismatch of the thermal expansion coefficients  between the polymer film and the silicon substrate and maybe further accelerated by higher thermal history and mismatch in the other physical properties (Young’ modulus and Poisson’ ratio). As shown in table 1., the PMDA-ODA polyimide prepared from each precursor exhibits the higher residual stress and thermal expansion coefficients than those of BPDA-PDA.

The corresponding value of residual stress in thin films were about 30MPa. However, BPDA-PDA polyimides prepared from PAA precursor give a significantly lower residual stress and thermal expansion coefficients than that does polyimide prepared from the other amic acid precursor as shown in Table 1. After the cure , the intrinsic stress in the resulting polyimide films was relatively small, regardless of precursors origin. As though observed on the semi-flexible PMDA-ODA polyimide, the BPDA-PDA polyimide showed significant dependency of the precursor origin on its stress-temperature profile.

The residual stress of PMDA-ODA film measured using the TFSMS equals the sum of thermal and intrinsic stresses, i.e.,

µ §	  															(2)

The thermal stress caused by the thermal expansion mismatch between film and wafer at two different temperature. The intrinsic stress is known to be resulted from volume change due tommolvent evaporation and shrinkage, from molecular structural ordering during the film formation process.

For PMDA-ODA PAA, the residual stress increases gradually with increasing curing temperature up to 350oC. Fig. 1 shows the stress-temperature profile of the polyimide film measured during heating to 150oC and subsequent cooling. On heating, intrinsic stress decrease from 16MPa at room temperature to 7MPa at 150oC. During aging at 150oC for 30min, the intrinsic stress increased from 7Mpa to 9.5Mpa . This stress increase might result from a morphological change due to molecular ordering occurred during the aging. However, stress is very sensitive to the amount of residual solvent, therefore, this stress increase might result partially from the removal of residual solvent. On cooling after bake, stress increased from 9.5MPa at 150oC to 24MPa at room temperature. Fig. 2 presents the stress-temperature profile of the film baked at 250oC for 30min. On heating, intrinsic stress decreased with temperature from 24MPa at room temperature to 2MPa at 250oC. During aging at 250oC for 30min, intrinsic stress increased slightly from 2MPa to 4MPa. This stress increase is much smaller than that of the film aged at 150oC. On cooling after the bake, stress increased linearly with decreasing temperature from 4MPa at 250oC to 27MPa at room temperature.  Fig. 3 shows the stress behavior of the film baked at 350oC. On heating, the intrinsic stress of 18MPa at room temperature decreased monotonously with temperature to 0.5MPa at 350oC. During aging at 350oC for 30min, stress did not increased from 0.5MPa at 350oC. That is, the aging effect is very small above 250oC. Therefore, aging effect on the stress of PMDA-ODA becomes significant at temperatures below 250oC. On cooling after baking at 350oC, overall stress increased rapidly with decreasing temperature to 30MPa at room temperature.

The thermal stress component in the film was estimated by subtracting the measured intrinsic stress form the measured overall stress. The thermal stress component became more pronounced by the elevation of bake temperature. The ssnal stress is higher than that of the films baked atnn50oC, or 250oC, indicating that the thermal stress component baaomes more significant in the film baked at a higher temperature.

Fig.4 shows the stress-temperature profiles of the resulting PMDA-ODA polyimide films prepared from the amic acid precursor. After thermal imidization until 400oC, stress at room temperature was about 28 MPa for  PMDA-ODA PAA. In cooling after cure, stress increased with decreasing temperature in all the polyimide films. The stress behavior upon repeated thermal cycling is reproducible and is approximately linear in temperature, suggesting the stress observed in thermal in origin.

Conclusion

The comparison of the thermal stresses indicates that  the residual stress  of a polyimide thin film is primarily dependent on imidization history, 150oC, 250oC, 350oC in semi-flexible PMDA-ODA and semi-rigid BPDA-PDA polyimides. The higher imidization temperature gives the higher residual stress on Si wafer substrate. The polyimide thin films  studied here, PMDA-ODA polyimide exhibits higher overall residual stress in spite of relatively low transition temperature. Therefore, thermal expansion coefficient increases in the order of PMDA-ODA>BPDA-PDA.

In addition, the PMDA-ODA polyimides is similar to that observed for the hinged structure. and the thermal expansion coefficient and thermal induced stresses were approximately the same regardless of precursor types. Whereas residual stress of a BPDA-PDA polyimide is dependent on the origin of precursor: poly(amic acid)(PAA), poly(amic ester)(PAE).

Comparison with residual stresses behaviors of these polyimides, it shows a good agreement between morphological results and residual stresses of polyimide films prepared from different precursors.

Reference

1. Haksoo Han, Ph.D dissertation. (1993)

2. Hyunsoo Chung, Jongchul Seo, Haksoo Han, Theories and applications of 	chemical

engineering, vol.2, No.2, pp2575-2578. (1996)

3. J. Brekner and C. Feger, “Curing Studies of a Polyimide Precursor.", J of  Polym. Sci. :Part

A: Polym. Chem., 25, 2005-2020 (1987)

4. M. Ree, Thomas L. Nunes and George Czornyj and Willie Volksen, “Residual stress

behaviour of isomeric PMDA-ODA  polyimides.” Polymer,  33, 1228-1236 (1992)

5. John C. Coburn, Michael T. Pottiger, Susan C. Noe, and Stephen D. Senturia, “Stress in

Polyimide Coatings.” Polymer,  32, 1271-1283 (1993)

6. Wortman, J.J. and R. A. Evans, 1965. “Young’s modulus, Shear Modulus, and Poisson ratio

in Silicon and Germanium.” J.Appl.Phys., 36: 153 (1964)

Acknowledgment

We would like to thank Korea Scienece and Engineering Foundation (96-0200-06-01-3) and  IITA(Institue of Information Technology Assessment, U96-141)for financial support of this work.

Polyimide

Precursor

Thickness

Residua

| l Stresses (micron) MPa BPDA-PDA Amic Acid 12 20 Amic Ester 10 27 PMDA-ODA Amic acid 11 | 30 |  | Amic Ester 10 31 Table 1. Designation of Polyimide Thin Film Structures and Measured Residual stresses at 25oC. µ §µ § Fig.1. Stress versus temperature behavior o |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |

f  PMDA-ODA   Fig.2. Stress versus temperature behavior of PMDA-ODA

during baking up 150oC and subsequent cooling.                   during baking up 230oC and subsequent cooling.

µ §µ §

Fig 3. Stress versus temperature behavior of PMDA-ODA           Fig.4. Residual stress behaviors of PMDA-ODA

during baking up 350oC and subsequent cooling                           polyimide on  Si wafer during curing process