격막 물질전달이 지배하는 활성탄-MSM 흡착계에서 흡착 특성

김성현, *이재욱, 문 희

전남대학교 응용화학 공학부, *서남대학교 화학공학과

Film-Diffusion Controlled Adsorption Characteristics

in Activated Carbon-MSM System

Kim Seoung Hyun, *Jae Wook Lee, Hee Moon

Faculty of Applied Chem. Eng., Chonnam National University, Kwangju 500-757

*Department of Chem. Eng., Seonam University, Namwon 590-711

## Introduction

In recent years, developing and applying efficient and cost-effective technologies for treatment of waters contaminated with synthetic organic chemicals (SOCs) have become important. Many synthetic organic chemicals (SOCs) present in drinking water are of major concern because of their potential mutagenicity, carcinogenicity, and/or toxicity. These compounds are continuously produced in the form of pesticides, herbicides, solvents and other products.  Synthetic organic chemicals (SOCs) could be introduced into drinking water by water runoff, through waste discharge, or by chemical spills. Under these circumstances the conventional solid/liquid separation technologies such as coagulation, sedimentation, and sand filtration have been employed for drinking water production.

Metsulfuron methyl(MSM) herbicides are widely used to control broad-leaved weeds in the world. However, these compounds are toxic and may persist in the environment for many months. After application they permeate into soil and can subsequently run off from cropland into rivers and lakes, causing surface water pollution. Removal of these potentially harmful compounds from water has emerged as an important issue of environmental protection.

The objectives of this study are to investigate the adsorption characteristics of MSM on activated carbon and to obtain the reliable information to be applied in analyzing and simulating the adsorption capacity of granular activated carbon (GAC) used in the synthetic organic carbon (SOCs) treatment system.

# Theoretical Model

Among well-known adsorption isotherms for single species, the Sips equation was used to fit experimental equilibrium data. The Sips adsorption equation is represented by

q=qmbC1n1+bC1n

where qm is the amount of adsorption and b and n are empirical constants of the Sips equation.

### Surface Diffusion Model

In the surface diffusion model, adsorption of adsorbates occurs at the outer surface of the particle, followed by diffusion of adsorbate molecules in the adsorbed state along the pore walls inside the particle. The driving force is the concentration gradient of the adsorbed adsorbate on the pore walls. A material balance for spherical particle results in the following mass transfer equations:

∂q∂t=1r2∂∂r(r2Ds∂q∂r)

kf(C−Cs)=Dsρp∂q∂r     at   r = Rp

∂q∂r=0    at r = 0

### Pore Diffusion Model

In the pore diffusion model, diffusion of molecules occurs in the pore fluid and adsorption takes place when molecules reach the adsorption sites. Based on the assumption of a spherical particle, dilute solution, and local equilibrium, the the adsorbate mass transfer equations are as follows:

εp∂Cp∂t+ρp∂q∂t=εpr2∂∂r(r2Dp∂Cp∂r)

kf(C−Cs)=εpDp∂Cp∂r    at   r = Rp

∂Cp∂r=0     at   r = 0

Cp=Cp0,  q=q0      at   t = 0

### CSTR(Continuous Stirred Tank Reactor) Model

A well-mixed tank is initially filled with a solution of volume V and concentration Cin, At time t≥0, fluid commences to flow in and out at a volumetric flow rate of v.

Unsteady state mass balance in a continuous-flow tank is given as follows:

VdCbidt=v(Cin−Cbi)−kfiS(Cbi−Cfi)

where kfi denotes the film mass transfer coefficient and Cbi , the concentration of bulk phase and Cfi the concentration at the particle surface.

# Experiment

# The different two type of activated carbon particle size was used. One was passed through 20 mesh and retained on 30 mesh (ASTM). The other one was passed through 16 mesh and retained on 20mesh(ASTM). The average particles diameter was estimated to be 0.84 and 0.59×10-3m from the sieve openings. The solution concentration of MSM was 0.05 mol/m3.

For batch kinetic experiments, about 0.05 mol/m3 stock solution of MSM was used and the rotation speed in the batch adsorber containing 2L solution was 500 rpm, 300 rpm, 200 rpm, 120 rpm, 50 rpm. Also, for continuous stirred tank reactor (CSTR) experiments, about 0.05 mol/m3 and 0.1 mol/m3 stock solutions was used and the volumetric flow rates of v were 3, 5, 7, 9 cc/min.

In order to obtain breakthrough curves of MSM, 0.05 mol/m3 stock solution was passed through a packed bed charged with activated carbon. All samples were analyzed by an UV spectrometry (Varian DMS100).

# Results and Discussion

Among well-known adsorption isotherms for single species, Sips equation was used to fit experimental equilibrium data. For MSM/AC systems, mass transfer mainly controlled by the film mass transfer. Therefore, CSTR or a fluidized bed rather than a fixed-bed adsorber should be used for the removal apparatus. The model proposed here can be used for simulating experimental data obtained in batch and CSTR adsorbers.

# Reference

1)  J. S. Kim, S. J. Lee, S. H. Yoon, and C. H. Lee: Competitive adsorption of trace organic

on membranes and powdered activated carbon in powdered activated carbon-

ultrafiltration system. Wat. Sci. Tech., 34, 223-229(1996).

2)  Najm, I. N., Snoeyink, V. L., Suidan, M.T., Lee, C. H. and Richard, Y.: Effects of particle

size and background natural organics on the adsorption efficiency of  PAC. J. AWWA.,

82,65-72(1990)

3)  Thomas F. Speth: Glyphosate removal from drinking water.

J. Env. Eng., 119, 1139-1157(1993).

Fig 1. Effect of RPM on Conc. Decay

Curves ( Particle size = 0.59 mm )

Fig 2. Effect of RPM on Conc. Decay

Curves ( Particle size = 0.84 mm )

Fig 3. Comparison of experimental data with simulated result for a CSTR run using the Surface Diffusion Model

( Initial conc. 0.05 mmol/L, 500 RPM )

Fig 4. Comparison of experimental data with simulated result for a CSTR run using the Surface Diffusion Model

( Initial conc. 0.1 mmol/L, 300 RPM )

Fig 5. Breakthrough curves of MSM in

terms of Bedlength with v=3 cc/min,

Initial conc. 0.05 mmol/L

Fig 6. Breakthrough curves of MSM in

terms of flow rate , Bedlength 7 cm,

Initial conc. 0.05 mmol/L