비 이온성 고분자 수지를 이용한 아미노산의 흡착

이재욱1, 정흥조1, 문 희2

서남대학교 화학공학과

전남대학교 응용화학공학부

Adsorption of Amino Acids on a Nonionic Polymeric Sorbent

Jae Wook Lee*, Heung Joe Jung*, Hee Moon**

* Department of Chemical Engineering, Seonam University, Namwon

** Faculty of Applied Chemical Engineering,Chonnam National University, KwangJu

INTRODUCTION

Amino Acids have an important role in many fields such as pharmaceutical, food, and health product industries. In early days, the production of amino acids was based on recovery from protein hydrolysates. However, presently they are produced by microbial fermentation processes. They are separated from the fermentation broth by complicated and costly ion-exchange schemes due to low concentration and very low solubility in organic media.

Ion exchange is widely used in a lot of stages of processes for industrial production of amino acids. Since amino acids called zwitterions exist both as anions and cations depending upon the solution pH, ion-exchange resins have been usually employed for the separation of them both in analytical scale and in industrial manufacturing processes [1,2]. Generally, adsorption and desorption in ion exchange resin systems may be induced by changing the solution pH [1]. Although adsorption capacities of nonionic polymeric sorbents are less than that of an ion exchanger, the desorption step may be easier and faster than the case when we employs an ion exchanger. Therefore, it is meaningful to investigate the adsorption equilibria, kinetics and column dynamics of amino acids in detail.

In this study, we measured equilibrium amounts of amino acids such as phenylalanine, tryptophan and tyrosin on a nonionic resin, SP850. The internal diffusion coefficient was obtained from the batch experiment. A simple dynamic model for fixed-bed adsorbers was formulated and solved by an orthogonal collocation method.

THEORY

A surface diffusion model with external mass transfer resistance was selected in this study because of its simplicity and adequecy in describing adsorption of amino acids from aqueous solution on a nonionic polymeric sorbent. The model was developed for an isothermal adsorption column, packed with porous spherical particles. The flow pattern is described by the axial dispersed plug-flow model. Other assumptions involved in the model include spherical adsorbent particles, isothermal condition and fast intrinsic adsorption kinetics, as well as local equilibrium between the solid-phase and liquid-phase solute concentrations at the surface of the particles. The diffusion inside a spherical adsorbent particle is described by the following equation:

∂qi∂t=Dsi∂2qi∂r2+2r∂qi∂r			(1)

The solute mass balance in the liquid phase is:

(2)

The adsorption isotherms of each species were represented by the Langmuir equation and the mutual competitive interaction between amino acids was expressed by the IAST(ideal adsorbed solution theory). The system of partial differential equations were numerically solved. Eqs. (1) and (2) were first discretized using an orthogonal collocation method [3]. By this method, the second-order partial differential equations are reduced to a set of first-order ordinary differential equations. The resultant equations were simultaneously integrated using an integrating package, LSODI of the International Mathematics and Science Library(IMSL).

EXPERIMENTAL

The nonionic polymeric sorbent used in this study was SP850, a macroreticular and spherical sulfonated polystyrene resin cross-linked with DVB(divinylbenzene) which was supplied by Mitzubishi Chemical Co. (Japan). The physical properties of SP850 are summarized in Table 1.

Prior to experiments, the sorbent was leached with isopropyl alcohol for 24 hours to wet internal pores. Sorbent particles were loaded in a 0.02 m ID glass column and a ten-bed volume of sodium hydroxide (0.1N) and HCl (0.1N) were passed through the column successively at a flow rate of 1.0 x 10-4 m3/min in order to remove impurities. Finally, a twenty bed-volume of distilled and deionized water was passed at the same flow rate to rinse off HCl. The amino acids encountered in this study were L-phenylalanine (Phe), L-tryptophan(Trp) and L-tyrosine(Tyr). These amino acids were obtained in crystalline forms from Sigma and used without further purification. The properties of amino acids are listed in Table 2.

Equilibrium experiments were carried out by contacting a given amount of sorbent with    amino acids solution of 1-30 mol/m3 and keeping in a constant temperature shaking incubator. After equilibrium was reached, the excess amino acid left in the solution was analyzed using a ultraviolet spectrometry (Varian DMS 100S) at 258, 280 and 275 nm for phe, tryp and tyr, respectively. The adsorption capacity of the resin was calculated from the material balance. Kinetic experiments for the determination of internal diffusivities are conducted under the condition of 500 rpm in a batch adsorber.

Dynamic adsorption experiments were carried out in a glass column of 0.01m diameter and 0.10m length, which was packed with resin particles. The column was lined with a water jacket to maintain a uniform column temperature.    The flow rate was regulated by a precision pump (Fluid Metering Inc., QSY).    The solution was introduced downward into the column. To prevent channeling and to enhance the flow distribution through the column, two layers of small glass beads were packed in the top and bottom regions of the column. Samples were withdrawn from the effluent line and were analyzed to get breakthrough curves.

Table 1. Properties of a Polymeric Sorbent, SP850

| Property | Values | Unit |
| --- | --- | --- |
| Particle diameter | 382 | μm |
| Particle density | 457 | kg/m3 |
| Moisture content* | 52 | % |
| Surface area* | 1,000 | m2/g |
| Average pore diameter* | 38.1 | Å |
| Pore volume* | 0.89 | cm3/g |

* From the manufacturer’s report

Table 2. Properties of Amino Acids used at 298K.

| Property | Phe | Trp | Tyr |
| --- | --- | --- | --- |
| Molecular form Solubility in Water (mol/m3) | C9H11NO2 29.6 | C11H12N2O2 12 | C9H11NO3 0.5 |
| Molecular weight | 165.19 | 204.23 | 181.19 |
| pK1 | 1.83 | 2.83 | 2.20 |
| pK2 | 9.13 | 9.39 | 9.11 |
| pK3 | - | - | 10.07 |
| pI | 5.48 | 5.89 | 5.66 |

RESULTS    AND    DISCUSSIONS

As illustrated in Fig. 1, adsorption amounts of phe on SP850 is greater than that of trp at 298K. The experimental data are well correlated by Sips equation. Fig. 2 shows the energy distribution curves in terms of r value, which is the isotherm parameter of Dubinin-Astakov equation. r has been used as a criteria of adsorption heterogeneity. This figure shows that the homogeneities of an adsorption system increased with the value of isotherm parameter, r. From the binary batch experiment, IAST can be used for describing competitive adsorption of phe and trp on a nonionic polymeric sorbent, SP850. As shown in Fig. 3, the proposed simple dynamic model incorporated with IAST can predict the binary adsorption breakthrough curves satisfactorily.

REFERENCES

1.    Saunders, M.S., Cierow, J.B. and Carta, “Uptake of Phenyalanine and Tyrosine by a

Strong-Acid Cation Exchanger”, AIChE J. (1989)

2.    Helfferich, F., “Ion Exchange Equilibrium of Amino Acids on Strong-Acids Resins :

Theory”, Reac. Polym., 12, 95 (1990)

3.    Villadsen, J. and Michelsen, M.L., Solutions of Differnential Equations Models

by Polynomial Approximation, Prentice-Hall, Inc., 1978

Fig 2. Effect of r on energy distribution curves at Eo=5kJ/mol

Fig 3. Experimental and simulated binary breakthrough curves

of Phe and Trp system

Fig 1. Single-species isotherms of Phe and Tryp on SP 850