- 고정층흡착탑에서 비이온성 고분자 흡착제를 이용한 아미노산의 흡착과 탈착특성

- 양우철, 고주영, 이재욱*, 문 희

- 전남대학교 응용화학부

*서남대학교 화학공학과

- Characteristics of Adsorption and Desorption of Amino acids on a Nonionic Polymeric Sorbent in Fixed-bed Adsorber

- Woo Chul Yang, Ju Young Ko,*Jae Wook Lee, Hee Moon

Faculty of Applied Chemistry, Chonnam National University, Kwangju 500-757

*Department of Chemical Engineering, Seonam University, Namwon 590-170

- Introduction

Amino acids and biochemicals have been important materials in many fields. These biochemicals are mainly produced by microbial fermentation processes. They are separated from the fermentation broth by complicated and costly ion exchange schemes due to low concentration and very low solubility in organic media. Such biochemicals are usually amphoteric. They exist both as anions and cations, depending upon the solution pH. Therefore adsorption and desorption of these biochemicals on ion-exchange resins may be carried out by adjusting the solution pH.

Ion-exchange has been the most widely used technology in various stages of the separation processes for industrial productions[1]. Although adsorption capacities of nonionic polymeric sorbents are less than those of ion exchangers, the desorption step may be easier and faster than the case when one employs an ion exchanger. Therefore, it is meaningful to investigate the adsorption equilibria, kinetics, and column dynamics of amino acid-nonionic polymeric resin systems in detail[2].

In this work, we investigated the fixed-bed adsorption and desorption characteristics of amino acids such as phenylalanine and tryptophan on a nonionic polymeric sorbent in terms of concentration, flow rate, and bed length. A simple dynamic model for fixed-bed adsorbers was formulated and solved by an orthogonal collocation method.

Theory

A surface diffusion model with external mass transfer resistance was selected in this study because of its simplicity and adequacy in describing adsorption of amino acids from aqueous solution on a nonionic polymeric sorbent. The model was developed for an isothermal adsorption column, packed with porous spherical particles. The flow pattern is described by the axial dispersed plug-flow model. Other assumptions involved in the model include isothermal condition and fast intrinsic adsorption kinetics, as well as local equilibrium between the solid-phase and liquid-phase solute concentrations at the surface of the particles. The diffusion inside a spherical adsorbent particle is described by the following equation:

∂qi∂t=Dsi∂2qi∂r2+2r∂qi∂r			(1)

The solute mass balance in the liquid phase is:

-DL∂2Ci∂z2+∂vCi∂z+∂Ci∂t+1−εbεb∂qi∂t=0

(2)

The adsorption isotherm of each species was represented by the Langmuir equation and the mutual competitive interaction between amino acids was expressed by the IAST(ideal adsorbed solution theory). The system of partial differential equations was numerically solved. Eqs. (1) and (2) were first discretized using an orthogonal collocation method [3]. By this method, the second-order partial differential equations are reduced to a set of first-order ordinary differential equations. The resultant equations were simultaneously integrated using an integrating package, LSODI of the International Mathematics and Science Library(IMSL).

- Experimental

The nonionic polymeric sorbent used in this study was XAD-16, a macroreticular and spherical polystyrene resin cross-linked with DVB(divinylbenzene) which was supplied by Rohm and Haas Co. (Spring House, PA).

The amino acids encountered in this study were L-phenylalanine(Phe) and L-tryptophan(Trp). These amino acids were obtained in crystalline forms from Junsei Chemical Co.(Japan) and used without further purification.

Dynamic adsorption experiments were carried out in a glass column of 0.015m diameter and 0.05~0.10m length, which was packed with resin particles. The column was lined with a water jacket to maintain a uniform column temperature.  The flow rate was regulated by a precision pump (Fluid Metering Inc., QSY).  The solution was introduced downward into the column. To prevent channeling and to enhance the flow distribution through the column, two layers of small glass beads were packed in the top and bottom regions of the column. Samples were withdrawn from the effluent line and were analyzed to get breakthrough curves. Fig.1 show the schematic diagram of an apparatus used for column experiments.

A UV spectrophotometry(Varian, model DMS 100s) with 1mm path length quartz cuvettes was used to determine the concentration of Phe and Trp at 254 and 275nm, respectively.

Fig. 1. Schematic diagram of an apparatus used for column operation

- Results and Discussion

- Fig. 2 show the effect of bed length on adsorption of Phe on XAD-16. The experimental results show that the breakthrough curve has a sharper shape when a shorter column used. Generally, this result can be observed when the column length is shorter than the zone length.

- Since the flow rate is a very important factor in fixed bed design, its effect should be checked. Fig. 3 show that the break time appeared earlier with higher flow rates. On the other hand, the breakthrough curves were steeper with higher flow rates. In general, if the flow rate was decreased or the bed length was increased, the breakthrough curve is becoming steeper. However the results obtained here show contrary tendencies, which can be explained by two reasons, the linear single component adsorption isotherm and the film mass transfer controlling. Fig. 4 also shows that breakthrough curves are not so influenced by initial concentrations since the isotherm is almost linear.

In general, there are many regeneration techniques such as thermal, steam, acid of base and solvent regeneration. The choice of a certain regeneration method will depend upon the physical and chemical characteristics of both the adsorbate and the sorbent. For nonionic polymeric sorbent, the solvent regeneration technique has been known to be superior to other methods since the attractive forces binding the solute to the resin surface are physical in nature. The solvent regeneration of polymeric sorbents is particularly effective when the components adsorbed are very soluble in the solvents. In many cases they penetrate the gel phase of the polymeric matrix. Fig. 5 show three desorption curves obtained with 10% aqueous solution of IPA, methanol, with only distilled, and deionized water, respectively.  The effect of methanol and IPA in desorption is qualitatively similar, but vary significantly in magnitude. As shown in Fig. 5, IPA is sufficient to desorb the amount of adsorption by the same extent as methanol. Even pure water without organic solvents was introduced into the column, Phe was desorbed quite well but it took longer to completely desorbe it.

## References

- Blackburn. S.,’Amino Acids and Amines”, Handbook of Chromatography, CRC Press, Boca Ration,(1983)

- Lee, J.W, Jung, H.J., and Moon, H., Adsorption of amino acids on nonionic polymeric sorbent,Theories and Application of Chem. Eng., 4(1),617(1998)

3.  Villadsen, J. and Michelsen, M.L., Solutions of Differnential Equations Models

by Polynomial Approximation, Prentice-Hall, Inc., 1978

FFig. 2. Effects of bed length on the

experimental results and model

predictions of breakthrough

curves for adsorption on XAD-16

FFig. 3. Effects of flow rate on the

experimental results and model

predictions of breakthrough

curves for adsorption on XAD-16

FFig. 5. The desorption curves for Phe

using organic solvents on  XAD-16

FFig. 4. Effects of concentration on the

experimental results and model

predictions of breakthrough

curves for adsorption on XAD-16

3

3

3