액정과 선형 고분자 혼합물의 상거동 : Extended Flory-Huggins 이론의 적용

이용석, 배영찬

한양대학교 응용화학공학부 분자열역학 연구실

## Phase Behaviors of Nematic Liquid Crystal / Linear Polymer Systems :

## Applicability of The Extended Flory-Huggins Theory

Yong Seok Lee, Young Chan Bae

Division of Chemical Engineering

And Molecular Thermodynamics Lab.

Hanyang University, Seoul 133-791, Korea

# Introduction

Phase behaviors of nematic liquid crystals (EBBA (P-ethoxy-benzylidene-p-n-butylaniline) and MBBA (P-methoxy-benzylidene-p-n-butylaniline)) in linear polystyrene ( PS ) are investigated by thermo-optical analysis ( TOA ) technique. We modify interaction parameter,χFH, to take into account both polymer concentration and temperature and develop a new model by combining Ballauff’s model with the extended Flory-Huggins model. The model used in this work includes two adjustable model parameters (d0,d1). Results are compared with the proposed model.

# Theory

 Ballauff model

The combinatorial analysis along the lines given by Flory may be readily adapted for the system under consideration. As usually, the mixing partition function ZM is subdivided into a combinatorial, an orientational, and a configurational part.

ZM=ZCombZOrientZConfig                                    (1)

whereZconfig is a constant. Thus, this treatment excludes the possibility of any ordering effect of the nematic phase on the polymer coils residing therein. The quantity y specifies the disorientation of the rodlike paritcles. For a molecule with the long axis at an angle ψ with respect to the domain axis.

y=4πxrsinψ                                      (2)

ZM=n0−nx(xr−y)!n0−nxxr!nx!n0nx(y−1)Zorientn0−nxxr!n0−nxxr−ncxc!nc!n0nc(xc−1)       (3)

The orientational partition function Zorient may be expressed as :

Zorient=Πyωynxnxyexp(−xrεy/2kBT)nxy                          (4)

εψ=−(kBTV)νrs(1−32sin2ψ)                                 (5)

Isotropic energetics may be included in the form of a characteristic temperature for an isotropic interaction and it is shown as :

ΔHM=ncxcvrTisoT=ncxcvrχ                             (6)

 The proposed model

Qian et al. and Bae et al proposed that χ is given by the product of a temperature-dependent term, D(T),  and a concentration-dependent term, B(νr)

χT,νr=D(T)B(νr)                                      (7)

D(T)=d0+d1T                                           (8)

B(νr)=11−bνr                                          (9)

where, d0,d1and b are adjustable model parameters. In this study, bis fixed a unity so that there are two model parameter in the proposed model.

 Chemical Potential

Anisotropic phase

Δμr'RT=lnνr'xrVr+νr'(y−1)+νc'xr1−VrVcxc+xrVrV'−1+xr(Vr−1)a+ln1−1V'

−lnf1−xrνr'sV'θ1−12s−12sνr'1−V'Vr+12sνc'

+d0+d1T11−bνr'2νcVrxrVc                        (10)

Δμc'/RT=lnνc'xcVc+νr'VcxcVrxr(y−1)+νc'VcVrxc−1+xcVc1V'−1Vr+Vcxca

d0+d1T11−bνr'2νcVrxrVc         (11)

Isotropic phase

Δμr/RT=lnvrxrVr+vr(xr−1)+vcxr1−VrVcxc+xrVV−1+xr(Vr−1)ln1−1V

+d0+d1T1−b1−bνr2νr2xc                            (12)

Δμc/RT=lnνcxcVc+νrVcxcVr1−1xr+νcVVrxc−1+xcVc1V−1Vr

+xcVc−1ln1−1V+d0+d1T1−b1−bνr2νr2xc           (13)

# Results and Conclusion

We proposed an improved thermodynamic model based on the extended Flory-Huggins theory to describe the phase behavior of nematic liquid crystal/linear PS systems. The model gives slightly better agreement with experimental data than that of Dorgan’s. It might be that we do not take into account all interactions that exist in the given systems, especially specific interactions between molecules. It is likely that the deficiency is basically responsible for the discrepancy between the proposed model and experimental data.

# References

1. P. J. Flory and G. Ronca, Mol. Cryst. Liq. Cryst. , 54 , 311(1979)

2. P. J. Flory and G. Ronca, Mol. Cryst. Liq. Cryst. , 54 , 289(1979)

3. M. Ballauff , Mol. Cryst. Liq. Cryst. , 136 , 175(1986)

4. J. R. Dorgan and D. S. Soane , Mol. Cryst. Liq. Cryst. , 188 , 129(1990)

5. P. J. Flory , Macromolecules , 11 , 1138(1978)

6. M. Ballauff and P. J. Flory , Ber. Bunsegas Phys. Chem. , 88 , 550(1984)

7. P. J. Flory and P. Irvine, J. Chem. Soc. Faraday Trans.I. , 80 , 1807(1984)

8. Y.C.Bae , J.J. Shim. D.S.Soane and J.M.Prausnitz, J. Applied Polymer Science,

47 , 1193~1206(1993)

9. C. Qian , S. J. Munby and B. E.Eichinger , Macromolecules , 24 , 1655(1991)

10. E. Kuss , Mol. Cryst. Liq. Cryst. , 47 , 71(1978)

Fig.4. The phase diagram of EBBA/PS (Mw=113,000) system. The solid line is the proposed model. Dotted line and dashed line are Dorgan’s model for T*iso=40.0 and 45.0, respectively.

Fig.2.The phase diagram of EBBA/PS

(Mw=56,000) system. The solid line is the proposed model. Dotted line and short dashed line are Dorgan’s model for T*iso=55.0 and 60.0, respectively.

Fig.3.  The phase diagram of EBBA/PS

(Mw=71,000) system. The solid line is the proposed model. Dotted line and dashed line are Dorgan’s model for T*iso=40.0 and 45.0, respectively

Fig.1.The phase diagram of EBBA/PS

(Mw=39,000) system. The solid line is the proposed model. Dotted line and dashed line are Dorgan’s model for T*iso=45.0 and 47.0, respectively.