- 개질화된 활성탄 컬럼에서 수증기와 유기용매 혼합증기의 동특성

- 이재욱, 이종원, 심왕근*, 이후근**, 문  희*

- 서남대학교 환경화학공학부

- *전남대학교 응용화학학부

**KAEL 환경연구원

Adsorption Dynamics for Water Vapor and Organic Chemicalsin

Modified Activated Carbon Column

- Jae Wook Lee, Jong Won Lee, *Wang Geun Shim, **Hoo Kun Lee, *Hee Moon

Faculty of Environmental & Chemical Engineering, Seonam University, Namwon *Faculty of Applied Chemistry, Chonnam National University, Kwangju     **KAEL Environmental R&D Center

### Introduction

A number of studies have been reported in the literature related to the water vapor adsorption mechanism and isotherms on activated carbon [1,2]. However, few research works on multicomponent adsorption under humid conditions have been studied [3,4]. Competitive adsorption between water vapor and organics can be considered a special case of multicomponent adsorption, because water vapor is nearly always present in gas streams and it exhibits much different adsorption characteristics on activated carbon than organics. Therefore, it is important to understand water vapor adsorption and its effects on activated carbon for the design and operation of adsorption processes. This research examines the effects of humid air on the adsorption dynamics in a fixed-bed column charged with a Cu/Cr/Ag impregnated activated carbon.

- Theoretical Model

The mathematical model for the process is a isothermal, dynamic-column adsorption process. The model adopted here utilizes the hybrid isotherm equation and a linear driving force (LDF) rate model to simplify the mass transfer inside adsorbent particles. Ideal gas law was also applied for the gas phase. The component mass balance can be expanded for a isothermal, isobaric process to give;

∂Xi∂t=DL∂2Xi∂z2−υ∂Xi∂z−1C1−εBεBρp⋅∂qi∂t−k∂qk∂t 		(1)

Mass transfer rates is expressed as a LDFA model:

∂qi∂t=ksiqi−qi						 (2)

The boundary conditions employed correspond to the Dankwert’s boundary conditions for the closed-closed system with no dispersion to the immediate left of  z=0 and to the immediate right of z=L. These coupled parabolic second-order partial differential equations, Eqs. (1) and (2), cannot be analytically. Therefore numerical methods have been generally employed. In this work, the coupled PDEs were first reduced to a set of ODEs by an orthogonal collocation method, and resultant ODEs were integrated with respect to time by using the subroutine LSODI. The linear algebraic equations arising from the discretized overall material balance was efficiently solved using LU-decomposition.

### Results and Discussion

Fig. 1 shows the adsorption capacity of water vapor measured at 308.15 K. The adsorption isotherms of water vapor on impregnated activated carbon was of Type V, according to Brunauer’s classification[4]. Isotherms play an important role in the prediction and design of adsorption systems. Thus, the careful selection of a single component isotherm depends on the concept of the accuracy and thermodynamic consistency of an isotherm model. The accuracy of an isotherm model is a function of the number of independent parameters. However, its popularity in relation to the process application is a function of mathematical simplicity. Only a few of many available isotherm models may be applied to water vapor adsorption, such as the well-known Dubinin-Serpinski (DS) equation. The original DS equation describes water vapor adsorption for the relative vapor pressure range from 0.0 to 0.6. Barton et al. extended it over the entire range of vapor pressure using an empirical four-parameter nonlinear equation. These isotherms have limitation for the analysis of adsorption dynamics, whereas the modified isotherm proposed by Qi et al. [5] has the advantages of expressing q explicitly as a function of P/P0 , containing three isotherm parameters (q0, k and P50)

q=q01+expkP50P0−PP0				(3)

The plot of Eq. (3) exhibits a characteristic S shape with P50 at q/q0=0.5 as an inflection point. The determined values by a nonlinear fitting method are q0=0.304, k=8.136, and P50/P0=0.586. The solid line in Figure 1 is the prediction result by Eq.(3) using these isotherm parameters. Fig. 2 shows the adsorption isotherm of acetone in terms of temperatures.

Fig. 1. Adsorption isotherm of water vapor.   Fig. 2. Adsorption isotherm of acetone.

Our ultimate goal of this study is for the prediction of multicomponent column  dynamics of between water vapor and organic gases on impregnated activated carbon adsorbent. In general, the isotherm types of both organic gases and water vapor on activated carbon are different. The former isotherm is favorable and the letter one is “S” shape isotherm. Thus, it is quite difficult how to combine each isotherm. For this purpose, multicomponent equilibium model should be required. There are a lot of models of multicomponent equilibria such as extended Langmuir equation, vacancy solution model, ideal adsorbed solution theory (IAST), and real adsorbed solution theory (RAST). Among them, IAST has been widely used for many adsorption systems since it has the advantages of goodness-of-fit isotherm data of multicomponent adsorption equilibria and only single-species isotherm parameters are needed in calculation procedure. The following equation is one of the governing equations for IAST as a candidate model for the multicomponent equilibrium prediction of water and organic vapors. In order to calculate multicomponent equilibria, the following equation should be evaluated.

Π≡πiART=qi0pi0dpi0				  (4)

Eq.(4) can be evaluated for the DS-1 and DS-2 [2] as follows;

Π=−q0c(PP0)ln(−P0+cP)+q0c(PP0)lnP		  (5)

Π=cP0(q0+q)(1−kq)P			       (6)

while it was impossible for DS-3 and Eq. (1). Although Eq. (1) has some advantages for the description of water vapor isotherm, it is impossible for the calculation of multicomponent equilibria.

Fig. 3. Breakthrough curves of CCl4 and acetone in terms of column length.

Fig. 4. Breakthrough curves of water vapor  Fig. 5. Binary breakthrough curves of

in terms of humidity (RH=20, 40, 65%).	        water and CCl4 at RH=35%.

Fig. 3 and 4 show the single-species breakthrough curves of acetone, CCl4, and water vapor. Fig. 5 show the binary breakthrough curve of water/carbon tetrachloride in impregnated activated carbon adsorber preloaded with water vapor at RH=70%. As one can be expect, the binary adsorption breakthrough curves are typical pattern under two different humidity conditions of RH =35% and RH=50%. However, the binary breakthrough curves of water/acetone vapors at RH=35% and somewhat lower RH=25%, showed abnormal behaviors. It was believed that carbon tetrachloride is coadsorbed after saturation stage based on the fact that acetone is water-soluble whereas carbon tetrachloride is water-insoluble. Further studies on multicomponent equilibria will be continued for precise quantitative prediction of the competitive adsorption phenomena between water vapor and organic chemicals of carbon tetrachloride and acetone by employing coadsorption theory.

REFERENCES

- Barton SS, Evans M.J.B, MacDonald J.A.F. The adsorption of water vapor by porous carbon. Carbon 1991; 29(8):1099-1105.

[2] Biron E, Evans. JBM. Dynamic adsorption of water-soluble and insoluble vapours on activated carbon. Carbon 1998; 36(7-8): 191-1197.

[3] McCallum CL, Bandosz TJ, McGrother SC, Muller EA, Gubbins KE. A molecular model for adsorption of water on activated carbon: comparsion of simulation and experiment. Langmuir 1999;15:533-544.

- Jeinen AW, Peters JA, Bekkum HV. Competitive adsorption of water and toluene on modified adsorption carbon supports. Applied Catalysis A 2000;193-202.

[5] Qi S, Hay KJ, Rood MJ. Isotherm equation for water vapor adsorption onto activated carbon. J Env Eng 1998;124(11):1130-1134.