마이크론 사이즈 젤 입자의의 상거동

홍 영표, 배 영찬

한양대학교 응용화학공학부 분자열역학 연구실

## Swelling behaviors of submicron sized hydrogel particles

Young Pyo Hong, Young Chan Bae

Div. of chemical Engineering and Molecular Thermodynamics Lab.

Hanyang University, Seoul 133-791, Korea

# Abstract

Temperature and ionic strength sensitive hydrogels play an important role in the application of pharmacy, medicine and separation operations in biotechnology.  The most important thermodynamic property of gel is the degree of swelling for application.  Thermodynamically, swelling behaviors of nonionic hydrogels were interpreted by the polymer-solvent mixing free energy and elastic free energy.

In this study, to successful prediction of nonionic hydrogels, we combined the Modified Perturbed Hard Sphere Model (MPHSC) and Flory and Erman‘s theory of elasticity. We used Modified PHSC developed by Chapman’s bonding term as the reference term and van der Waals attractive term as the perturbation. Our proposed model shows good agreements with experimental PVT data water and gel swelling data.

# Theory

At equilibrium, the chemical potential μ of every component i is the same in both phases

μi′=μi″

Where single prime and double prime represent the gel phase and the external phase of the gel, respectively.  In the solvent, equation (1) becomes at equilibrium state

μ1−μ10=Δμ1=Δμ1,mix+Δμ1,ela=0

1. Mixing contribution

The general PHSC equation of state folloews1, 2

PρkT=PρkTref.+PρkTpert.

The modified PHSC3, 4, 5with van der Waals perturbation term expressed as

PρkT=1+r2bρgd+−r−1ρ∂lngd+∂ρ−r2aρkT

where P is the pressure, ρ=N/V is the number density (N is the number of molecules and V is the volume), and k is the Boltzmann’s constants. The number of segments (effective hard spheres) per molecule is represented by r, gd+ is the radial distribution function of hard spheres at contact and d is the hard sphere diameter. a and b reflects the attractive forces between two non-bonded segments and the van der Waals covolume per segment or the second virial coefficient of hard spheres, respectively. Theses values are temperature dependent.

aT=2p3s3eFakT/e

bT=2p3d3T=2p3s3FbkT/e

with

FakT/εii=1.8681exp−0.0619kT/εii+0.6715exp−1.7317kT/εii3/2

FbkT/εii=0.7307exp−0.1649kT/εii1/2+1−0.7303exp−2.3973kT/εii3/2

The equation of state for the mixtures are obtained by extending pure equation

PρkT=1+ρijmxixjrirjbijgijdij+−imxiri−1ρ∂lngiidii+∂ρ−ρkTijmxixjrirjaij

where xi=Ni/N is the number fraction of molecules, ri is the number of hard spheres, and gijdij+ is the pair radial distribution function of hard-sphere mixtures at contact.6

gijh,xij=11−h+32xij1−h2+12xij21−h3

where h and xij are as followed

h=ρ4imxiribi

xij=bibjbij1/3ρ4kmxkrkbk2/3

These variables are segment density ρr=Nr/V, and segment fraction fi=Niri/V, where Nr is the total number of segments in the system of which the volume is V.

The general equation for calculating the Helmholtz energy from an equation of state is7

AT,V,Ni=imAi0T+P−NkBTVdV+kBTimNilnNkBTV

The chemical potential of component k in multi component systems

μkkT=μk0kT+2rkρrimφibi1Wik+ρrijmφiφjbijNr∂Wij∂Nk−rk−10ρr∂lngkk∂ρrdρr−imφi1−1rirk∂∂φk0ρr∂lngii∂ρrdρr−2rkρrkTimφiaik+lnφkrkρrkT+1

where

Nr∂Wij∂Nk=∂Wij∂ηkNr∂η∂Nk+∂Wij∂ξijNr∂ξij∂Nk

2. Elastic Contribution

For a perfect tetrafunctional network, Flory and Erman obtain the chemical potential due to elastic forces8.

Δμ1,elakT=φgo2xCλ−11+B[B(1+B)−1+(λ/κ)2(B+λ2B)(1+λ2B/κ)−1]

where

B=∂B/∂λ2=B[(λ2−1)−1−2(λ2+κ)−1]

with

B=λ2−1(1+λ2/κ)2

λ is the linear swelling ratio

λ=VV013=φg0φg13

where V and V0 are the volume of the gel network and the volume in the reference state, respectively. φg and φg0 are the corresponding volume fractions of the gel. The characteristic parameter κ relates xC and φgo as follows:

κ=14PφgoxC1/2

Here the dimensionless parameter P depends on characteristics of the generic type of polymer and the molar volume of solvent. We set P to a unity. And xC is the average chain length between cross-linking points

# Conclusion

We used modified PHSC model to predict the swelling behaviors of submicron size particle gels. Model parameters of water obtained from PVT data of water. Two binary model parameters were calculated from the liquid-liquid equilibrium (LLE) data of PNIPA/water system showing LCST behavior, which were directly used to describe the swelling behaviors of NIPA hydrogel systems.

The swelling curves calculated from the proposed model agrees fairly well with the experimental data with two adjustable model parameters.

# References

[1] Y. Song, S. M. Lambert and J. M. Prausnitz, Chem. Eng. Sci.. 1994, 49, 2765

[2] Y. Song, S. M. Lambert and J. M. Prausnitz, Ind. Eng. Chem. Rds., 1994, 33, 1047

[3] I. H. Kim, Y. C. Bae, Polymer, 2000, 41, 875

[4] I. H. Kim, Y. C. Bae, Fluid Phase Equilibria, 2000, 168, 201

[5] W. G. Chapman, G. Jackson, K. E. Gubbins, Mol. Phys. 1988, 65, 1057

[6] T. Boublik, J. Chem. Phys. 1970, 53, 417

[7] J. M. Prausnitz, R. N. Lichtenthaler, E. G de Azevedo, Molecular Thermodynamics of Fluid Phase Equilibria, 3rd edition, Prentice-Hall, Englewood Cliffs, NJ, 1998

[8] B. Erman, P. J. Flory, Macromolecules, 1986, 19, 2342