공압출 유동에 대한 삼차원 수치모사: 실험결과와의 비교

선우기병, 안경현, 이승종

서울대학교 응용화학부

Three-Dimensional Numerical Simulation of Coextrusion Flow:

Comparison with Experimental Data

Ki Byung Sunwoo, Kyung Hyun Ahn, and Seung Jong Lee

School of Chemical Engineering, Seoul National University, Seoul 151-744, Korea

Introduction

Coextrusion is the simultaneous extrusion of two or more layers of different materials through a common die. This process provides superior products by combining the unique properties of different resins and offers economic advantages.

White et al. [1] applied the theory of nonlinear viscoelastic fluids to consider stress and velocity profiles and interface shape in stratified flow, and showed that the fluid with the greater absolute second normal stress difference tends to protrude into the other fluid. Southern and Ballman [2] investigated the relative importance of viscosity and elasticity effects on the interface shape. Karagiannis et al. [3] studied isothermal generalized Newtonian coextrusion process using a three-dimensional analysis and compared with the experimental results. Takase et al. [4] performed a three-dimensional numerical simulation with viscoelastic model and showed that the encapsulation phenomena were affected not only by viscous properties but also by elastic or non-linear properties. Sunwoo et al. [5] implemented the open boundary condition method to remove the ambiguity of outlet boundary conditions in three-dimensional numerical simulation of viscoelastic coextrusion process.

In this work, to compare our numerical results with the experimental data reported in Karagiannis’ study [3], we used generalized Newtonian fluid, the Giesekus model, and two-mode Phan-Thien and Tanner model. After fitting the parameters of constitutive equations using the shear viscosity data only, we will compare the numerical results with the experimental coextrusion data.

Governing equations and Numerical methods

In this study, the problem consists of the merging flow of two fluid streams and the interface shape development in the resulting bicomponent stratified flow inside the die.

Assuming incompressible, steady state flow with no body forces, the three-dimensional forms of continuity and momentum equations for the flow of two fluids (I and II) are

∇⋅vk=0, 				k=I, II		  (1)

ρkvk⋅∇vk=−∇pk+∇⋅τk			k=I, II		  (2)

and the boundary conditions at the interface are expressed as followings.

kinematic conditions :

n⋅vI=n⋅vII=0,	(3)

t1⋅vI=t1⋅vII,	(4)

t2⋅vI=t2⋅vII	(5)

dynamic conditions :

t1⋅σI=t1⋅σII,	(6)			t2⋅σI=t2⋅σII,	(7)

n2⋅σI−n2⋅σII=0	(8)

For the shear rate dependency of shear viscosity in generalized Newtonian fluids, Carreau model is used, which is written as,

η(IIΔ)=ηo 1+λIIΔ2122n−12	(9)

As viscoelastic constitutive equations, we used the Giesekus model [6], which is written as,

τ=τp+2ηsD,						(10)

τp+λ1τ∇p+αλ1ηpτp2=2ηpD,				(11)

and two-mode Phan-Thien and Tanner (mPTT) model [7], which is written as,

τ=i=12τi,						(12)

(1+εiλiηo,itrτi)τi+λi(1−ξi2)τi∇+ξi2τiΔ=2ηo,iD		(13)

The flow domain is discretized into 27-node hexahedron elements as shown in Fig.1, and the Galerkin finite element procedure is applied. Zero shear viscosity ratio (o,II /o,I) and flow rate ratio (QII/QI) are 2.5 and 13.2, respectively.

Results and Discussion

The Carreau model for shear rate dependency of generalized Newtonian fluid was employed to fit the shear viscosity data of two polystyrenes (Fluid I and Fluid II) used by Karagiannis et al. [3]. The interface position around the symmetric plane obtained by numerical simulation nearly coincided with the one observed in experiment by Karagiannis et al. [3], but the degree of encapsulation (DE(%)= yw−yc/L×100) was less than the one observed experimentally as shown in Fig. 2.

For the Giesekus model, we fitted the shear viscosity data by nonlinear fitting algorithm (Marquardt-Levenberg algorithm) after fixing α to 0.15 or 0.30. Fitted viscosity curves using αvalue as 0.15 or 0.30 nearly coincide with the experimental shear viscosity curves. For two-mode Phan-Thien and Tanner (mPTT) model, we did the similar procedure as Giesekus model, but the fitted viscosity curves are not as smooth as that of Giesekus model.

As α ratio (αFluid I : αFluid II) between Fluid I and Fluid II increases from 1.0 (0.3:0.3) to 4.0 (0.4:0.1), and as 1 ratio (1 Fluid I : 1 Fluid II) increases from 1.0 (0.3:0.3) to 3.0 (0.54:0.18), the degree of encapsulation along the downstream direction increased as represented in Figures 3 and 4. The α of the Giesekus model represents the second normal stress difference as 1 of mPTT model does, so we can guess that the second normal stress difference has a great influence on the gradual increase of the degree of encapsulation along the downstream direction. There was little difference between numerical results and the experimental data in the interface profile and the degree of encapsulation along the downstream direction when α ratio and 1 ratio were set to 3.0.

We have fitted parameters of viscoelastic constitutive equations using the shear viscosity data only. So, if we can get the accurate second normal stress difference data, we can evaluate the accuracy of our numerical results more precisely.

References

- White, J. L., R. C. Ufford, K. R. Dharod, and R. L. Price, J. Appl. Polym. Sci., 16, 1313 (1972).

- Southern, J.H. and R. L. Ballman, J. Polym. Sci., 13, 863 (1975).

- Karagiannis, A., A. N. Hrymak, and J. Vlachopoulos, Rheol. Acta, 29, 71 (1990).

- Takase, M., S. Kihara, and K. Funatsu, Rheol. Acta, 37, 624 (1998).

- Sunwoo, K.B., S. J. Park, S. J. Lee, K. H. Ahn, and S. J. Lee, J. Non-Newtonian Fluid Mech., (submitted).

- Giesekus, H., J. Non-Newtonian Fluid Mech., 11, 69 (1982)

Fig. 2. Interface profile at z/L=8.0 with generalized Newtonian fluid.

Phan-Thien, N. and R. I. Tanner, J. Non-Newtonian Fluid Mech., 2, 353 (1977).

Fig. 3. Degree of encapsulation along the downstream direction with the Giesekus model.

Fig. 1. Finite element mesh (Mesh1).

II

2L

z/L=13.48

L

z=0

z/L=4.0

z/L=7.16

I

Fig. 4. Degree of encapsulation along the downstream direction with mPTT model.